| Name | No Cells | Positive electrode | Negative Electrode | Nominal Capacity (Ah) | Temperature (oC) |
| --- | --- | --- | --- | --- | --- |
| HUST (18650 cylindrical) | 77 | LFP | Graphite | 1.1 | 30 |
| MATR (18650) | 169 | LFP (LiFePO4) | Graphite | 1.1 | 30 |
| CALB | 27 | NMC | Graphite | 58 | 0, 25, 35, 45 |
| ISU (502030 Li-polymer) | 240 | NMC (lithium nickel manganese cobalt oxide) | Graphite | 0.25 | 30 |
| MICH_EXP (pouch) | 12 | NMC (NMC111) | Graphite | 5.0 | -5, 25, 45 |
| MICH | 40 | NMC (NMC111) | Graphite | 2.36 | 25, 45 |
| RWTH | 48 | NMC (lithium nickel manganese cobalt oxide) | Carbon | 3 | 25 |
| SDU (18650) | 86 | NMC | Graphite | 2.4 | 25 |
| STANDFORD (18650) | 41 | NMC (LiNi0.5Mn0.3CoO.2O2) | Graphite | 0.24 | 30 |
| STANDFORD 2 (18650) | 181 | NMC LiNi0.5Mn0.3CoO.2O2 | Graphite | 0.24 | 30 |
| XJTU | 23 | NMC LiNi0.5CoO.2Mn0.3O2 | Graphite | 2 | 20 |
| TONGJI (18650 cylindrical) | 108 | NCA / NMC blend (LiO.86NiO.86CoO.11AlO.03O2 and LiO.84(NiO.83Co0.11Mn0.07)O2) | Graphite | 2.5 and 3.5 | Multiple (no info) |
| CALCE | 13 | LCO (LiCoO2) | Graphite | 1.1 | 25 |
| HNEI |  | LCO + NMC (LiCoO2 and LiNiO.4CoO.4Mn0.2O2) | Graphite | 2.8 | 25 |
| UL (18650) | 10 | LCO + NMC (LiCoO2 and LiNiO.4CoO.4MnO.2O2) | graphite | 3.4 | 23 |
| SNL (18650) | 52 | LFP + NCA + NMC (LiFePO4, LiNiO.81CoO.14AlO.5O2, and LiNiO.84Mn0.6Co0.O2) | Graphite | 1.1 and 3.2 and 3.0 | 15, 25, 35 |
| NA-ION (18650) | 31 | Na-ion | - | 1.0 | 25 |
| ZN-COIN | 95 | Zn-MnO2 (MnO2) | Zinc | 10 | 25 |

Group:

- LFP

  - HUST

  - MATR

- NMC

  - CALB

  - ISU

  - MICH_EXP

  - MICH

  - RWTH

  - SDU

  - STANDFORD

  - STANDFORD 2

  - XJTU

- LCO

  - CALCE

- Mix-Chemical

  - SNL

  - HNEI

  - UL

  - TONGJI

- Rest

  - NA-ION

  - ZN-Coin

Seperate – Together – whole

50 epochs x10